## Slide 1: Time-resolved scattering
Paul G. Evans
pgevans@wisc.edu
August 11, 2016

## Slide 2: Motivations: Timescales of Dynamical Processes
Atomic, molecular physics
Chemistry, chemical physics
Condensed matter, materials
Time (s)
10-15
10-12
10-9
10-6

## Slide 3: Examples of Dynamical Phenomena in Condensed Matter 1
GHz Mechanical Materials and Devices
Fundamental Excitations
- Structure and Dynamics of Excitons in Organic Semiconductors
- Phonon Generation and Dynamics
THz Electronics and THz Properties of Materials
Marciniak et al., Phys. Rev. Lett. 99, 176402 (2007).
Rinaldi et al., IEEE Trans. on Ultrasonics, Ferroelectrics, and Freq. Control 57, 38 (2010).
B. Ferguson and X.-C. Zhang, Nature Mater. 1, 26 (2002).

## Slide 4: Examples of Dynamical Phenomena in Condensed Matter 2
Magnetic Dynamics: Spin-transfer Torque
Dynamics in Complex Oxides
Atomic and Thermal Transport
- Pulsed Laser Materials Processing
- Nanomaterials Thermal Transport
Pribiag, et al., Nature Phys. 3, 498 (2007).
M. A. Scarpula, et al., Appl. Phys. Lett. 82, 1251 (2003).
N. A. Spaldin and M. Fiebig, Science 309, 391 (2005).

## Slide 5: Small and Fast Go Together
Small and fast
  If you want to look at dynamical processes in small areas you need to be fast
  If you want to look at small areas the dynamics can be fast.
  1 km/sec = 1 nm/ps (~sound)
  (108 m/sec=100 nm/fs)
Timescales/wavelengths of probes must be chosen to match the problem.
X-rays (wavelength ~ 1 Å) match the size-scale of atomic-to-nanoscale processes.
Many ways to use x-rays to study dynamics.

## Slide 6: What about Bandwidth?
Question: Can we just find a way to chop up x-rays and do the same experiments we’d do with longer pulses? At synchrotrons: yes.
The energy bandwidth and duration of optical pulses are related by an uncertainty relation called the time-bandwidth product: ΔE Δt > h
A 2 fs visible pulse with λ=600 nm has a bandwidth of nearly 300 nm, spanning nearly the whole visible spectrum.
X-rays have far higher frequency, and the same frequency width is not a concern, even for fs pulses.

## Slide 7: X-ray Sources are Not Yet Transform Limited
Synchrotron Radiation Light Sources
  Example:
    APS 100 ps duration pulse, 100 eV bandwidth from undulator, typical 1 eV bandwidth selected for diffraction.
    ΔE Δt =30000 h (!!!)
Free Electron Lasers
  LCLS and other FELs based on spontaneous emission are closer, but not there yet.
So far, just use the pulsed x-ray sources as short duration lamps.

## Slide 8: How Close are FELs? Really Close!
J. Amman et al., Nature Photonics 6, 693 (2012).
LCLS normal operation: SASI, several modes
LCLS self seeding test 0.5 eV bandwidth at 8 keV

## Slide 9: What if we were at the transform limit?
Dixit et al., Proc. Nat. Acad. Sci. 109, 11636 (2012)
We don’t have to worry about this in experiments yet!
Theory of scattering with transform-limited pulses from electron orbital wavepackets.

## Slide 10: Key Parameters and Sources of Short-Duration X-ray Pulses
Experimental design parameters: pulse duration, x-ray photon energy, repetition rate, photons per pulse
Synchrotron light sources
  40-100 ps duration, 100 eV-50 keV, MHz-GHz repetition rates, 103-107 photons/pulse
  (*) Also laser slicing sources, etc. for niche applications with short durations but very low flux.
Free electron lasers
  LCLS ~100 Hz repetition rate, 800 eV-8 keV, 2 fs, >1010 photons/pulse
  European XFEL: similar, but with ~30 kHz repetition rate

## Slide 11
D. Tiede (ANL)

## Slide 12: Experimental Strategies 1: Diffraction from Thin Films
Excite sample with a short transient, e.g. a laser pulse
Repeat diffraction experiment at a series of times.
H. Wen et al., Laser-driven strain in BiFeO3 thin flims, Phys. Rev. Lett. 110, 037601 (2013) and Phys. Rev. Lett. 112, 097602 (2014).

## Slide 13: Experimental Strategies 2: Solution Scattering
D. Tiede (ANL)

## Slide 14: Ultrafast Spectroscopy
X-ray absortion spectroscopy in solution.
Picosecond resolution using streak camera detector.
B. Ahr et al., Phys. Chem. Chem. Phys. 13, 5590 (2011).

## Slide 15: Examples of Experiments
Condensed Matter and Materials Science
Chemical Transformations
Biological Molecules

## Slide 16: Example 1: Dynamics in artificial ferroelectrics: ferroelectric/dielectric superlattices
Electronic properties arise from the E-field driven reconfiguration of domains.
Probing ultrafast structural dynamics is crucial. Future sources will provide insight into the mechanism of switching and the field-distorted structure of the superlattice.
SrO
PbO
SrO
TiO2
TiO2
TiO2
TiO2
TiO2
TiO2
TiO2
PbO
…
…
PbTiO3
12 unit cells
SrTiO3
3 unit cells
Self-organized nm-scale domains
J. Y. Jo, et al., Phys. Rev. Lett. 107, 055501 (2011).

## Slide 17: Time-Resolved Diffraction: SrTiO3/PbTiO3

## Slide 18
Nanodiffraction at APS sector 7: 100 nm spot size, ~100 ps time resolution

## Slide 19: Domains
Zubko, et al., Phys. Rev. Lett. 104, 187601 (2010)

## Slide 20: Domain Diffuse Scattering in 12(PbTiO3)/3(SrTiO3)
Domain period 9.5 nm
Coherence length only 20 nm

## Slide 21: No Piezoelectric Expansion within Domains
Domain wavevectors
In-plane
Out-of-plane

## Slide 22: Proposed Switching Mechanism
Challenges: 2D (or 3D) imaging of domains? During switching?

## Slide 23: Timescales for Structural Phase Transitions
Strain drives a transition between rhombohedral-like and tetragonal-like phases – and causes huge distortion.
What are the dynamics of these structural transitions? Expect that it proceeds at the sound velocity, ~1 nm/ps.
Pump with THz radiation, probe with X-ray pulses.
“Morphotropic” phase boundary in BiFeO3
R. J. Zeches, et al., Science 326, 977 (2009).

## Slide 24: Ultrafast Optical Excitation
Synchronize femtosecond laser with x-ray pulses
Laser specs: 400 nm (above bandgap)
50 fs duration
5 kHz repetition
2.5 W max power

## Slide 25: Ultrafast Strain Generation in BiFeO3
½% strain develops within 100 ps, relaxes in several ns
Minor thermal contribution to the peak strain, important at long times
Electronic contribution at short times, relaxation agrees with carrier recombination
H. Wen et al., Phys. Rev. Lett. 110, 037601 (2013).

## Slide 27: (Nearly) Instantantaneous Stress Generation
Strain consistent with elastic response to instantaneous stress.
D. Schick et al., Phys. Rev. Lett. 112, 097602 (2014).

## Slide 28: Example 2: Ultrafast Mechanics
4.5 GHz NEMS resonator
Rinaldi et al., IEEE Trans. on Ultrasonics, Ferroelectrics, and Freq. Control 57, 38 (2010).
11 GHz whispering gallery mode resonator
M. Tomes and T. Carmon, Phys. Rev. Lett. 102, 113601 (2009).
High Q and high frequency are desirable but highly challenging in materials and device design.
What are the mechanical modes?
Where does nonlinearity come from?
100 ps is not fast enough to capture the relevant effects.

## Slide 29: Ultrafast Coherent Diffraction Imaging of Strained Nanostructures
Time zero
Time +50ps
(002) peak
Ni-capped ZnO nanorod coherent diffraction
R. Harder (ANL)

## Slide 30: Acoustic Modes of Nanocrystals
J. N. Clark et al., Science 341, 56 (2013).

## Slide 31: Imaging Phase Transformations
VO2 low-temperature insulating monoclininc phase, high temperature metallic rutile phase
Y. Zhu et al., Scientific Rep. 6, 21999 (2016).

## Slide 32: Example 3: Tracking phonons in time and momentum
Phonon-phonon, electron-phonon interactions
Time-domain often necessary to access these non-equilibrium states
Future sources will match x-ray scattering to the natural timescale of these interactions.
Nonthermal distributions, anharmonic decay
M. Trigo, et al., Phys. Rev. B, 82 235205 (2010).
A. Debernardi, et al., Phys. Rev. B., 57, 12847 (1998).
Ultrafast thermal diffuse scattering

## Slide 33: Fourier Transform Methods for Phonon Dispersions
Femtosecond laser impulsive excitation.
Diffuse scattering oscillates, Fourier transform to determine phonon frequency.
M. Trigo et al., Nature Phys. 9, 790 (2013).

## Slide 34: Time Dependence of Diffuse Scattering
Depends on Phonon Dispersion
Determine two parameters:
1) q from location in reciprocal space
2) Ω from time dependence
M. Trigo et al., Nature Phys. 9, 790 (2013).

## Slide 35: Experimental Phonon Dispersions
M. Trigo et al., Nature Phys. 9, 790 (2013).
Ge

## Slide 36: Example 4: Imaging Microscopic Multiphase Liquid Flows
Can high-speed flows (often turbulent) be a well-controlled process?
Engine sprays, high-pressure industrial sprays. Immediate implication for next-generation fuel and combustion.
Spray direction
Humberto Chaves (Freiberg U)
Challenges:
Optically dense due to many interfaces
Highly dynamic – high temporal resolution
Even more difficult on micrometer length scale-high spatial resolution
X-rays provide easily interpreted image of mass density.
High-pressure injector
High-pressure diesel spray
Jet with in-nozzle vorticity
Liquid drop bouncing on a solid surface
J. Wang (ANL)

## Slide 37: Examples of Experiments
Condensed Matter and Materials Science
Chemical Transformations
Biological Molecules

## Slide 38: Example 1: Photo-decomposition of Iodomethane
D. Tiede (ANL)

## Slide 39: Example 2: Molecular Excited States
D. Tiede, L. Chen (ANL)

## Slide 40: Example 2 (continued): Molecular Excited States
D. Tiede, L. Chen (ANL)

## Slide 41: Examples of Experiments
Condensed Matter and Materials Science
Chemical Transformations
Biological Molecules

## Slide 42: Example: Photo-deligation in Myoglobin
D. Tiede (ANL)
Cho et al., Proc. Nat. Acad. Sci. 107, 7281 (2010).
Start in carbon monoxy form (MbCO), optically induced transition to deoxy form (Mb).

## Slide 43: Example: Photo-deligation (continued)
D. Tiede (ANL)
Cho et al., Proc. Nat. Acad. Sci. 107, 7281 (2010).

## Slide 44: New Strategies: Single-Shot Experiments at FELS
FELs have sufficient intensity that the sample can be damaged or destroyed by the first pulse! (Each LCLS pulse has the photons of 103-105 synchrotron bunches, but in 2 fs.)
Can you get the information you need in one pulse?
Can the pulses be short enough to get the information before the structure explodes?
Prediction (2000): Neutze et al. Nature 406, 752 (2000).

## Slide 45: Femtosecond Nanocrystallography
Experiment (2011)

## Slide 46: X-ray Nonlinear Optics

## Slide 47: New Sources are Coming Soon
Improvements in synchrotron sources
New FELs
  Building/Built: SACLA (Japan), European XFEL, Pohang (Korea), Swiss FEL
  LCLS-II (high-repetition rate)
Proposed FELs
  Hard x-ray LCLS upgrade

## Slide 49: Current and Future FELs

## Slide 50: Storage Ring Sources

## Slide 51: Conclusions
Dynamics in condensed matter, materials science, chemistry, and macromolecules have wide relevance to important questions.
X-ray techniques can address these questions using dynamical versions of techniques we’re familiar with.
Near Future: Many new sources, new techniques.
Further Future: Transform-limited x-ray pulses.