## Slide 1
Coherent Diffraction Imaging
Ross Harder
Compact Objects (CDI)
Non-compact samples (Ptychography)
Acknowledgments:
Prof. Ian Robinson (BNL)
Dr. Xiaojing Huang (BNL)
Dr. Jesse Clark (PULSE institute, SLAC)
Prof. Oleg Shpyrko (UCSD)
Dr. Andrew Ulvestad (ANL - MSD)
Dr. Ian McNulty (ANL – CNM)

## Slide 2: X-rays, two extremes for structural study:
X-ray Diffraction
(Scattering)
Is particularly sensitive to periodicity in the sample (Crystals)
Atomic resolution (unit cell)
X-ray Imaging
(Shadowgraphs)
Inhomogeneous,
non-periodic materials
Limited spatial resolution
(~0.001 mm)
Von Laue, Nobel 1914
Bragg & Bragg, Nobel 1915
Roentgen, Nobel 1900
Coherent Imaging
is scattering
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 3: Imaging regimes with coherent x-rays
absorption radiograph
phase contrast
in-line holography
coherent diffraction
X-ray beam
Kagoshima (1999)
Miao (1999)
Jacobsen (1990)
2a
z >> a2/l
z ~ a2/l
near-field Fresnel
far-field Fraunhofer
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 4: Refractive index and contrast in the x-ray region
Absorption contrast:
sensitive to Im(n)
Phase contrast:
sensitive to Re(n)
Diaz, Ana, et al, 2012. “Quantitative X-Ray Phase
Nanotomography.” Physical Review B 85.

## Slide 5: Refractive index and contrast in the x-ray region
Absorption contrast:
sensitive to Im(n)
Phase contrast:
sensitive to Re(n)
A. Diaz,et al., Journal of Structural Biology, vol. 192, no. 3, pp. 461–469, Oct. 2015.

## Slide 6: Polarized x-rays give sensitivity to electron spin
Figueroa, A. I., et al. (2014). Physical Review B, 90(17), 174421
in PtCo
LCP @ 11.565keV
RCP @ 11.565keV
Notes: Dichroism: difference in absorption depending on polarization of incident light due to
fine-structure splitting of electronic states (spin-orbit coupling).
Circular dichroism: differential absorption using left and right-circularly polarized light.

## Slide 7: CDI in Bragg geometry: Imaging displacement field (strain)
Displacement field u(r):
Coherent X-ray Diffraction measures:
Strain is a gradient of u(r), the phase component of the complex-valued density

## Slide 8: Coherence
Visibility of fringes is a direct measure of the coherence of a beam.
If beam is coherent across the spacing of the slits a Fourier Transform
of the slit structure is created downstream.

## Slide 9: Coherence
longitudinal coherence


transverse coherence
d
wc
z

## Slide 10: Coherence
longitudinal coherence


transverse coherence
d
wc
z

## Slide 11
Coherence: Laser Speckle
Laser Speckle: Interference pattern arising from randomly distributed scatterers
A. L. Schawlow “Laser Light" Scientific American, 219 (3), p. 120, (1968)
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 12: Simplest Speckle Experiment: Twinkle, Twinkle Little Star
Stars are big, but very far away. As a result, their light has a high transverse coherence.
As the light propagates through the atmosphere our eye detects a portion of
the coherent diffraction
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 13
K. Exner: Sitzungsber. Kaiserl.
Akad. Wiss. (Wien) 76, 522 (1877)
First Speckle: Exner, 1877
(using candle light)
M. von Laue: Sitzungsber. Akad. Wiss. (Berlin) 44, 1144 (1914)
First Speckle Photo:
von Laue, 1914
(using arc discharge lamp)
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 14
First X-ray Speckle:
M. Sutton et al., Nature 352, 608-610 (1991)
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 15: Why use synchrotron radiation?
Synchrotron sources offer:
Brightnesss (small source, collimated)
Tunability (IR to hard x-rays)
Polarization (linear, circular)
Time structure (short pulses)
Source brightness is the key figure of merit for coherent imaging
B = photons/source area, divergence, bandwidth
Fc ~ 2 B
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 16: Coherent X-ray References
Vartanyants, I A, and A Singer. 2010 “Coherence Properties of Hard X-Ray Synchrotron Sources and X-Ray Free-Electron Lasers.” New Journal of Physics 12 (3): 035004.
Singer, Andrej, and Ivan A Vartanyants. 2014. “Coherence Properties of Focused X-Ray Beams at High-Brilliance Synchrotron Sources.” Journal of Synchrotron Radiation 21 (1). International Union of Crystallography: 5–15. doi:10.1038/nnano.2008.246.
Nugent, Keith. 2009. “Coherent Methods in the X-Ray Sciences.” Advances in Physics 59 (1): 1–99. doi:doi: 10.1080/00018730903270926.

## Slide 17: Traditional Microscopy:
Lens-less Imaging:
Object Plane
Detector Plane
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 18: First demonstration of CDI with x-rays
diffraction pattern
J. Miao, Nature 400, 342 (1999)
reconstruction
Courtesy Prof. Oleg Shpyrko (UCSD)

## Slide 19: Coherent Diffractive Imaging:
Y. Takahashi et al.,
Phys. Rev. B 82, 214102 (2010)

## Slide 20: Large-format, single-photon sensitive x-ray CCD cameras opened the door to coherent x-ray imaging
Fairchild Peregrine 486 CCD Camera
• 4K x 4K pixel array (61.4 mm square area)
• 15 μm pixels, 100% fill factor
• Back-illuminated for up to 80% QE
• Readout noise < 5 e- at 50 Kpixels/s
• Dynamic range > 86 dB in MPP
• 6 s readout with four on-chip amplifiers
• Pixel binning for more rapid readout
• Peltier-cooled to -50 C for low dark current
Notes: 20

## Slide 21
Hi Resolution Imaging (CCD)?
210nm
At APS 34-ID-C:
9.25 hours of scanning
38 minutes of x-ray exposure
~7nm data
Rainbow color map (still) considered harmful
http://ieeexplore.ieee.org/document/4118486/

## Slide 22: Pixel array detectors: revolutionizing coherent imaging
Pilatus 6M detector
(PSI/Dectris)
D. Schuette, S. Gruner (Cornell)
PADs can be read out in ~1 ms
(CCDs take seconds!)
PAD pixels are 55-150 µm.
(CCDs are 12-24 µm)
Notes: 22

## Slide 23
Hi Resolution Imaging (PAD)?
700nm gold crystal
3 degree rocking curve
25 minute measurement
45 sec movie (3X APS-U measurement)
Quad Timepix GaAs sensor

## Slide 24
Coherent Diffraction from Crystals
|Fourier Transform|2

## Slide 25
H
K
|Fourier Transform|2
Coherent Diffraction from Crystals

## Slide 26
Measuring 3D CXD
kf
ki
CCD
Silver Nano Cube (111)
Q=kf-ki
Yugang Sun and Younan Xia, Science 298 2177 (2003)

## Slide 27
3D Ag Nano Cube
Yugang Sun and Younan Xia, Science 298 2177 (2003)
200nm
Q

## Slide 28
APS 34-ID-C
Precision scanning stage

## Slide 29: Original Phase Retrieval Paper (by D. Sayre):
NOT r=r2 Acta Cryst. (1952). 5, 60

## Slide 30
Critical sampling
Nyquist Freq = 1/(2*bandwidth)
Intensity is under sampled
N unknown densities
N/2 equations

## Slide 31
Oversampling 2x
N/2 equations
N/2 Unknown densities
N/2 Known Densities(zero)

## Slide 32
Reciprocal Space Constraints
Experimental Amplitudes
Oversampled
Thresholded
&
ZeroPadded
Direct Space Constraints
Support
Total Energy
Mixing previous iterates.
Positivity
J. R. Fienup Appl. Opt. 21 2758 (1982)
Collins Nature 298, 49 (1982)
R. W. Gerchberg and W. O. Saxton Optik 35 237 (1972)
Fienup, James R. 2013. “Phase Retrieval Algorithms: a Personal Tour.” Applied Optics 52 (1): 45–56.
Input Output Algorithms
FFT
FFT -1

## Slide 33
Reciprocal Space Constraints
Experimental Amplitudes
Oversampled
Thresholded
&
ZeroPadded
Direct Space Constraints
Support
Total Energy
Mixing old and new iterates.
Positivity
Input Output Algorithms
u(n)
t(n)
J. R. Fienup Appl. Opt. 21 2758 (1982)
Collins Nature 298, 49 (1982)
R. W. Gerchberg and W. O. Saxton Optik 35 237 (1972)
Fienup, James R. 2013. “Phase Retrieval Algorithms: a Personal Tour.” Applied Optics 52 (1): 45–56.

## Slide 34
Reciprocal Space Constraints
Experimental Amplitudes
Oversampled
Thresholded
&
ZeroPadded
Direct Space Constraints
Support
Total Energy
Mixing old and new iterates.
Positivity
Input Output Algorithms
Error Reduction
Hybrid Input-Output
u(n)
t(n)
J. R. Fienup Appl. Opt. 21 2758 (1982)
Collins Nature 298, 49 (1982)
R. W. Gerchberg and W. O. Saxton Optik 35 237 (1972)
Fienup, James R. 2013. “Phase Retrieval Algorithms: a Personal Tour.” Applied Optics 52 (1): 45–56.

## Slide 35
Reciprocal Space Constraints
Experimental Amplitudes
Oversampled
Thresholded
&
ZeroPadded
Direct Space Constraints
Support
Total Energy
Mixing old and new iterates.
Positivity
Harder, R., Liang, M., Sun, Y., Xia, Y., & Robinson, I. K. (2010). Imaging of complex density in silver nanocubes by coherent x-ray diffraction. New Journal of Physics, 12(3), 035019.
Huang, X., Harder, R., Xiong, G., Shi, X., & Robinson, I. (2011). Propagation uniqueness in three-dimensional coherent diffractive imaging. Physical Review B, 83(22), 224109.
Input Output Algorithms
Hybrid Input-Output
u(n)
t(n)

## Slide 36
Reciprocal Space Constraints
Experimental Amplitudes
Oversampled
Thresholded
&
Zero Padded
Direct Space Constraints
Support
Total Energy
Mixing previous iterates.
Positivity
Input Output Algorithms
u(n)
t(n)
Harder, R., Liang, M., Sun, Y., Xia, Y., & Robinson, I. K. (2010). Imaging of complex density in silver nanocubes by coherent x-ray diffraction. New Journal of Physics, 12(3), 035019.
Huang, X., Harder, R., Xiong, G., Shi, X., & Robinson, I. (2011). Propagation uniqueness in three-dimensional coherent diffractive imaging. Physical Review B, 83(22), 224109.

## Slide 37
3D Ag Nano Cube
Yugang Sun and Younan Xia, Science 298 2177 (2003)
200nm
Q

## Slide 38
2mm
Nature Materials 9, 120 - 124 (2010)
3D Strain Map in ZnO

## Slide 39
Nature Materials 9, 120 - 124 (2010)
3D Strain Map in ZnO

## Slide 40
Nature Materials 9, 120 - 124 (2010)
3D Strain Map in ZnO

## Slide 41
Patterned Gold Nanocystal Samples

## Slide 42
Multiple reflection reconstructions
11-1
1-11
-111
(11-1)
Notes: -*here is a movie of a 3D diffraction pattern along with a Scanning electron micrograph of the 200nm crystal being measured*
-this is the 11-1 Bragg peak from this crystal
-*you can see a defect of some kind which visible in this SEM image*
-possibly as a result of a slip band which has produced a ridge on the surface
-*Again you can see the characteristic fringes corresponding the facets of the crystal

## Slide 43
-π/2 π/2
11-1
11-1
1-11
-111
(11-1)
Multiple reflection reconstructions
Notes: -*here I’ve replaced the movie with a cut through the centre of the diffraction pattern with a logarithmic scale to allow for the high dynamic range of the image*
-*this image shows the reconstructed complex amplitude from this Bragg reflection.*
-twinning in reconstructions in an inherent problem – 50% of the time the complex conjugate of the solution will be found, but in this case easy to determine which orientation is up due to very obvious top and bottom facet
-The agreement with the SEM is uncanny, except interestingly there is no evidence of the defect in the reconstruction. This will be explained on the next slide
-*the next image shows the inverse Fourier transform of recovered phase information from this reflection with the arrows pointing in direction of q vector*
-this image reveals any displacement from the equilibrium lattice
-method is mostly sensitive to displacements in the direction of the Q vector
-as we can see there some displacement at the left corner of the crystal likely due to interactions between it and the substrate

## Slide 44
11-1
1-11
-111
(11-1)
(-111)
Multiple reflection reconstructions
Notes: -*here is another diffraction pattern of different reflection from the same crystal this time from -111*
-you can see that this diffraction pattern is not as perfect in its appearance – there are twin fringes which correspond to a defected region of crystal or a twin
-when we take a look at the reconstructed complex amplitude and recovered phase information the result of these twin fringes on reconstruction can be seen

## Slide 45
-π/2 π/2
-111
11-1
1-11
-111
(-111)
Multiple reflection reconstructions
Notes: -the defected region visible in the SEM image is clearly apparent in the reconstructed amplitude and phase
-there is a displacement either side of the defect which is likely associated with the crystal being stretched as a result of the different thermal expansion rates between Au and silicon substrate
-we now believe the defect is as a result of a section of reverse stacking with a slip line on either side of it. It is likely that there are also edge dislocations within the missing piece
-the reason that the first reflection does not show any evidence of the defect is that the Q vector of the 11-1 is perpendicular to direction of slip

## Slide 46
11-1
1-11
-111
(1/3 1/3 5/3)
Multiple reflection reconstructions
(1/3 1/3 5/3)
Notes: -it is possible to measure reflection from missing chunk and these are reconstructed amplitudes from the 1/3 1/3 5/3 reflection which corresponds to the missing section of crystal

## Slide 47
(-111)
11-1
1-11
-111
(1/3 1/3 5/3)
(1/3 1/3 5/3)
Multiple reflection reconstructions
Notes: -it is possible to measure reflection from missing chunk and these are reconstructed amplitudes from the 1/3 1/3 5/3 reflection which corresponds to the missing section of crystal

## Slide 48
(020) (-111) (11-1)
Multiple reflection reconstructions
Notes: -here are three images of the recovered phase which show distortion given by phi=q.u(r)
-Ions displaced from the ideal lattice result in a phase shift of phi in reflected wave from distorted region
-when phase is reconstructed a component of the phase is obtained in the direction of the q vector
-multiple Bragg reflections therefore give multiple components of the displacement vector from which we can construct a displacement field
-Three non-coplanar reflections are required to do this

## Slide 49
Produced by combining reconstructions from (11-1) (020) (-111)
Vector Displacement Field of Gold lattice

## Slide 50: BCDI Today
Operando Nanoscale Imaging
Ulvestad, A., et al. (2015).
Science, 348(6241), 1344–1347
Dislocation dynamics in Li-Ion battery
Liquid Catalysis
F. Hofmann, et al.
Sci Rep, vol. 7, p. 45993, Apr. 2017.
Strain Tensor Imaging
Dislocation dynamics in the hydriding phase transformations of Pd
Ulvestad, et al.
Nature Materials, vol. 16, no. 5, pp. 565–571, Jan. 2017.
A. Ulvestad, et al.
J. Phys. Chem. Lett., vol. 7, no. 15, pp. 3008, Aug. 2016.

## Slide 51: Imaging Lattice Dynamics Laser Pump – CXD Probe
ZnO CXD
(002) peak
Dufresne, E. M., Chollet, M., Harder, R., Leake, S., et al.
(2011). Nucl Instrum Meth A, 649(1), 191–193.
Diffraction pattern
as a function of laser
delay.
fast period = 400ps
slow period = 5.56ns

## Slide 52
Imaging Lattice Dynamics Laser Pump – CXD Probe@LCLS
Crystal A
101 ps and 241 ps
Crystal B
90 ps and 256 ps
600 pm “breathing modes”
Ultrafast three dimensional imaging of lattice dynamics in individual gold nanocrystals
J. N. Clark, L. Beitra, G. Xiong, A. Higginbotham, D. M. Fritz, H. T. Lemke, D. Zhu,
M. Chollet, G. J. Williams, M. Messerschmidt, B. Abbey, R. J. Harder,
A. M. Korsunsky, J. S. Wark & I. K. Robinson. (2013). Science, 341(6141), 56–59

## Slide 53
Ultrafast three dimensional imaging of lattice dynamics in individual gold nanocrystals
J. N. Clark, L. Beitra, G. Xiong, A. Higginbotham, D. M. Fritz, H. T. Lemke, D. Zhu,
M. Chollet, G. J. Williams, M. Messerschmidt, B. Abbey, R. J. Harder,
A. M. Korsunsky, J. S. Wark & I. K. Robinson. (2013). Science, 341(6141), 56–59
Imaging Lattice Dynamics Laser Pump – CXD Probe@LCLS

## Slide 54
Imaging Lattice Dynamics Laser Pump – CXD Probe@LCLS
Orthogonal slices
Through crystal density
MD simulation
at +110ps
Ultrafast three dimensional imaging of lattice dynamics in individual gold nanocrystals
J. N. Clark, L. Beitra, G. Xiong, A. Higginbotham, D. M. Fritz, H. T. Lemke, D. Zhu,
M. Chollet, G. J. Williams, M. Messerschmidt, B. Abbey, R. J. Harder,
A. M. Korsunsky, J. S. Wark & I. K. Robinson. (2013). Science, 341(6141), 56–59

## Slide 55
Ptychography
“Arbitrary” field of view
Quantitative phase information
Simultaneous image of sample illumination
Coherent Imaging of Extended Samples
Rodenburg, J., et al. (2007). Physical review letters, 98(3), 034801.
Thibault, et al. (2008). Science, 321(5887), 379–382.
29nm pixels

## Slide 56: Ptychography Microprobes -> Coherent Imaging Instrument
Vine, et al. (2012). Opt. Express, 20(16), 18287–18296.

## Slide 57: GdFe layered magnetic films
Ta (20 Å)
↓ Gd (4.5 Å)
↑ Fe (4.1 Å)
↓ Gd (4.5 Å)
↑ Fe (4.1 Å)
↓ Gd (4.5 Å)
↑ Fe (4.1 Å)
Ta (20 Å)
Si3N4
 101
A. Tripathi, O.S. et al., Proc Natl Acad Sci USA 108, 13393 (2011)

## Slide 58: Magnetic Contrast Mechanism
10-2 nm-1
Off-resonance:
On-resonance:
Gd M5 edge
A. Tripathi, O.S. et al., Proc Natl Acad Sci USA 108, 13393 (2011)
Notes: Fig. 2

## Slide 59: Real Space Reconstruction
Magnetic structure
(exit wave)
Illumination Function
A. Tripathi, O.S. et al., Proc Natl Acad Sci USA 108, 13393 (2011)

## Slide 60
Magnetic structure
(exit wave)
Illumination Function
A. Tripathi, O.S. et al., Proc Natl Acad Sci USA 108, 13393 (2011)
Real Space Reconstruction

## Slide 61
A. Tripathi, O.S. et al., Proc Natl Acad Sci USA 108, 13393 (2011)

## Slide 62: Increasing Field
d
a
c
e
d
c
c
b
a
96.5 mT
76.5 mT
58.5 mT
42.5 mT
7.5 mT
Ms
-Ms
A. Tripathi, O.S. et al., Proc Natl Acad Sci USA 108, 13393 (2011)

## Slide 63
Nanoscale Strain in SiGe
film devices
Hruszkewycz, S. O., Holt, M. V., et al. (2012). Nano Letters, 12(10), 5148–5154.

## Slide 64: Surface diffraction Coherent Imaging
Image local surface structure
Steps and step dynamics during film growth or interfacial reactivity
Nanoparticle nucleation
Defect distributions, particularly at interfaces
Combined with x-ray micro fluorescence…..
C. Zhu, et al. Applied Physics Letters, vol. 106, no. 10, p. 101604, Mar. 2015.

## Slide 65
Use of the Advanced Photon Source was supported by the U. S. Department of Energy, Office of Science, Office of Basic Energy Sciences, under Contract No. DE-AC02-06CH11357.
Strain in ZSM-5 Zeolite
Calcium Oxalate in
maize stover
Thank You
Scientific reports, 3, 2843. (2013)