## Slide 1
Scientific Achievement
Significance and Impact
Research Details
The work performed at High Flux Isotope Reactor’s HB-3A instrument, Oak Ridge National Laboratory was sponsored by the Scientific User Facilities Division, Office of Basic Energy Sciences, U.S. Department of Energy (DOE)
Spin Reorientation and Magnetism in Yb14-xPrxMnSb11
An abnormal peak is observed in the dc magnetic susceptibility of Yb13.47Pr0.53MnSb11. Neutron diffraction clearly indicates that this peak is caused by a spin re-orientation of Mn moments, which is consistent with results of magnetization measurements. Refinement on the data collection also shows that moments on Mn are ordered and that moments on Pr are not.
This work demonstrates the effect of trivalent rare earth substitutions on the magnetism of Yb14MnSb11 system. Comparing all the results of Yb14-xRExMnSb11, light rare earth substitutions and heavy rare earth substitutions lead to distinguished magnetic properties.
Neutron diffraction intensity of different indexes on different compositions shows no spin reorientation in Yb14-xPrxMnSb11 when the Pr amount is low and a spin reorientation when the Pr amount is high. Refinement on the data collection also shows that Mn has an ordered moment of 4 μB and that Pr has no ordered moments.
Yufei Hu, Chih-Wei Chen, Huibo Cao, Farkhod Makhmudov, Jason H. Grebenkemper, Makhsuda N. Abdusalyamova, Emilia Morosan, Susan M. Kauzlarich, Tuning Magnetism of [MnSb4]9- Cluster in Yb14MnSb11 through Chemical Substitutions on Yb sites: the Appearance and Disappearance of Spin Reorientation. Journal of the American Chemical Society doi:10.1021/jacs.6b05636. (2016).
a) Neutron diffraction intensities of the (004) and (400) of Yb14-xRExMnSb11 scanned over temperature. b) Temperature-dependent magnetic susceptibility and c) field-dependent magnetization at 5 K of Yb13.47Pr0.53MnSb11. d) Plot showing the spin reorientation.