## Slide 1: Exploring the Nanoworld with Small-Angle Scattering
Dale W. Schaefer, Professor Emeritus
Chemical and Materials Engineering
University of Cincinnati
Cincinnati, OH 45221-0012
dale.schaefer@uc.edu
Basic Concepts
Why do Small-Angle Scattering?
Imaging vs. Scattering
Basic Concepts
  Scattering Vector, Fourier Trns.
  Scattering Length Density
Particle Scattering
  Guinier Approximation
  Porod’s Law
Fractal Structures
Composite Materials
SAXS & SANS: θ < 6°
XRD
SAS
Source of x-rays, light or neutrons

## Slide 2: Crystals: Bragg’s Law and the scattering vector, q
θ
d
Ordered Structures give peaks in “reciprocal” Space.
Large structures scatter at small angles.
The relevant size scale is determined by 2π/q
q is a vector, determined by machine geometry
You can’t always determine the real space structure from the scattering data.
Problem: Nanomaterials are seldom ordered
SAXS: θ < 6°
real space
source
detector
Reciprocal space
q
Notes: "square" is related to the "phase problem." Not really a problem. For ordered systems we want to know the real-space structure. Not necessarily true for disordered systems.
Bragg's law includes a vector. Pole parallel to q.

## Slide 3: Disordered Structures in “Real Space”
10µm
Agglomerates
Primary Particles
Aggregates
Precipitated Silica
(NaO) (SiO2)3.3 + HCl —> SiO2 + NaCl
10 nm
Water Glass
Complex
Hierarchical
Disordered
Difficult to quantify structure from images.
Notes: We don't really want to know all the positions.

## Slide 4: Hierarchical Structure from Scattering
100,000 nm
200 nm
0.5 nm
10 nm
Agglomerate
Aggregate
Primary
Particle
Network
“Polymer”
Four Length Scales
Four Morphology Classes
Exponents related to
morphology
10
-7
10
-6
10
-5
0.0001
0.001
0.01
0.1
1
10
Intensity
-4.0
-2.0
-3.1
R
G
= 89
μ
q [Å-1] ~ Length-1 ~ sin(θ/2)
USAS
SAS
Real
Space
Reciprocal
Space

## Slide 5: Why Reciprocal Space?
10 µm
Isotactic polystyrene foams prepared by TIPS
Jim Aubert, SNL
Ultra-small-angle neutron scattering: a new tool for materials research. Cur. Opinion Sol. State & Mat Sci, 2004. 8(1): p. 39-47.
Images miss similarity

## Slide 6: Adding up the Phases (Assume x-rays)
Electron density distribution
n(r) = number of electrons in a volume element dr = dx dy dz around point r.
Scattering length density distribution
ρ(r) = scattering length in a volume element dr = dx dy dz around point r.
ρ(r) = bn(r)
Many electrons
Amplitude is the Fourier transform of the SLD distribution (almost)
r2
r3
r4
r1
scattering length of one electron
Wave scattered from one electron
Notes: 1 occurs because one particle is at the Origin, which need not be the case.

## Slide 7: Scattering Length Density (SLD) Distribution
Wave amplitude is the
Fourier transform of
the scattering length
density distribution
Can’t be measured
ρ(r)
What we measure: Square of the Fourier transform of the SLD distribution
Can’t be inverted
Scattered Intensity

## Slide 8: Characterizing Disordered Systems in Real Space
r
Real space
Electron Density Distribution
Correlation Function of the
Electron Density Distribution
Depends on latitude and longitude.
Too much information to be useful.
Depends on separation distance.
Retains statistically significant info.
r
Resolution problems at small r
Opacity problems for large r
2-dimensional
Operator prejudice
Throw out phase information
×
Problems with real space analysis
r
ξ
Notes: It would be difficult to live in a world where eyes were sensitive to phase. Be careful what you wish for.

## Slide 9: Imaging vs. Scattering
r
q
Real space
Reciprocal space
ξ
2π/ξ
Schaefer, D. W. & Agamalian, M. Ultra-small-angle neutron scattering: a new tool for materials research. Curr Opin Solid St & Mat Sci 8, 39-47, (2004).
Pegel, S., Poetschke, P., Villmow, T., Stoyan, D. & Heinrich, G. Spatial statistics of carbon nanotube polymer composites. Polymer 50, 2123-2132, (2009).

## Slide 10: Correlated Holes

## Slide 11: SAXS of Anodized Aluminum
Hu, N. et al. Interfacial morphology of low-voltage anodic aluminium oxide. J Appl Crystallogr 46, 1386–1396 (2013).

## Slide 12: Scattering from Spherical Particle(s)
2R
ρo
v = particle volume
I(q) ~ N(ρ - ρo)2v2P(q)
solvent SLD
Form Factor
N particles
Notes: ----- Meeting Notes (3/17/12 17:23) -----
Which cross section is this? What are the Units
----- Meeting Notes (3/17/12 17:29) -----
I(0) very sensitive to the large particles. Based on Bragg principles where would small particles show up.

## Slide 13: Particles in Dilute Solution
ρ1
ρ2
RV
R
1 particle

## Slide 14: Small-Angle Scattering from Spheres
Large object scatter at small angles
Silica in Polyurethane
AFM
Guinier Regime
Porod (power-law) Regime
Diameter = 140 Å
3 mm
Petrovic, Z. S. et al. Effect of silica nanoparticles on morphology of segmented polyurethanes. Polymer 45, 4285-4295, (2004)

## Slide 15: Guinier Radius
Initial curvature is a measure of length
Rg ~ π/q
Derived in 5.2.4.1
Notes: Rg = moment of inertia

## Slide 16: Guinier Fits
Notes: Logx =(ln x)/2.303
print (ln(360)-ln(50))/9.5e-4
2077.98
print sqrt(3*2077)
79 Å

## Slide 17: Dense packing: Correlated Hard Spheres
Packing Factor = k = 8 ϕ
Packing Factor ≅ 6
ξ
R
Å
Å
Notes: ----- Meeting Notes (3/17/12 17:44) -----
Calculation in Extras

## Slide 18: Colloidal Silica in Epoxy
500 Å
EPON 862 + Cure W+ Silica
Chen, R.S. et al, Highly dispersed nanosilica-epoxy resins with enhanced mechanical properties Polymer, 2008. 49(17): p. 3805-3815.
R=60 Å
Notes: The composite matrix analyzed in this work is Epon 862 epoxy
resin (diglycidyl ether of bisphenol F epoxy, Shell Corporation)
cured with EpiCure-W(diethyl diamino toluene, Shell Corporation).
Both materials were purchased from Miller-Stephenson Chemical
Company, Inc. In the remainder of this work, we refer to the cured
epoxy system (epoxy ?cure agent) as Epon862/W. This resin system
has been studied for aerospace applications due to its high
working temperature, good properties, and low viscosity [27].
These properties are all significant when resin-transfer molding
advanced carbon-fiber-reinforced composites.

## Slide 19: Disordered Structures in “Real Space”
10µm
Agglomerates
Primary Particles
Aggregates
Precipitated Silica
(NaO) (SiO2)3.3 + HCl —> SiO2 + NaCl
10 nm
Water Glass
Complex
Hierarchical
Disordered
Difficult to quantify structure from images.
Notes: We don't really want to know all the positions.

## Slide 20: Using RG: Agglomerate Dispersion
Light Scattering
sonicate
hard agglomerate
dry
3.5 µm
D.W. Schaefer, D. Kohls and E. Feinblum, Morphology of Highly Dispersing Precipitated Silica: Impact of Drying and Sonication. J Inorg Organomet Polym, 2012. 22(3): p. 617-623.)

## Slide 21: Beyond RG: Power-Law Scattering
100,000 nm
200 nm
0.5 nm
10 nm
Agglomerate
Aggregate
Primary
Particle
Network
“Polymer”
Four Length Scales
Four Morphology Classes
Exponents related to
morphology
10
-7
10
-6
10
-5
0.0001
0.001
0.01
0.1
1
10
Intensity
-4.0
-2.0
-3.1
R
G
= 89
μ
q [Å-1] ~ Length-1 ~ sin(θ/2)
USAXS
SAXS

## Slide 22: Mass-Fractal Objects
Mass Fractal Dimension = d
Real Space
M~Rd
Dispersion
d = 3
d ≅ 2.5
M ~V ~ R3
M ~V ~ R2
M ~V ~ L1
M ~V ~ R2.2

## Slide 23: Surface Fractal Dimension
S ~ Rds
S ~ R2
fractal or self-affine surface
Sharp interface
2 < ds < 3

## Slide 24: Porod Slope for Fractals
Structure
Dimensions
Porod Slope= ds – 2dm
dm = 3
d
s
= 2
- 4
dm = 3
2 < d
s
≤ 3
- 3 ≥ Slope ≥ - 4
1 ≤ ds = dm ≤ 3
- 1 ≥ Slope ≥ - 3
Smooth Surface
Rough Surface
Mass Fractal
I(q)=qds-2dm

## Slide 25: Scattering from colloidal aggregates
R
r
Precipitated Silica
Log q
Log I
qR = 1
qr = 1
q-d
q-4

## Slide 26: Morphology of Dimosil® Tire-Tread Silica
Two Agglomerate length Scales
Soft = Physically Bonded
Hard = Chemically Bonded
2
-4
7 µm
116 µm
300 nm
Light Scattering
USAXS
126 Å
Dispersion
Reinforcement
Schaefer, D. W., Kohls, D. & Feinblum, E. Morphology of Highly Dispersing Precipitated Silica: Impact of Drying and Sonication. J Inorg Organomet Polym 22, 617–623 (2012).
Notes: ----- Meeting Notes (3/17/12 17:53) -----
Same light scattering data.

## Slide 27: Aggregates are robust
Soft Agglomerates
Hard Agglomerates
Aggregates
What is the ideal aggregate size?
shear
Ragg

## Slide 28: Conclusion
If you want to determine the morphology of a disordered material
use small-angle scattering.
Tomorrow
Nature at the Nanometer Level: SAXS of composites

## Slide 29: Scattering from Fractal Objects: Porod Slopes
d = Mass Fractal Dimension
ds = Surface Fractal Dimension
Match at qR = 1
qR = 1
Large q
~ Sv/q-x
Small q

## Slide 30: Differential Scattering Cross Section
sample
dΩ
θ = scattering angle
Plane wave J0
Spherical wave JΩ
Spherical wave: Flux JΩ = energy/unit solid angle/s or photons/ unit solid angle /s
Plane wave: Flux J0 = energy/unit area/s or photons/unit area/s

## Slide 31: What do we really measure?
length
Area
beam
Scattering cross section depends on sample size: Bad
Often called the scattering cross section or the intensity