## Slide 1
Scientific Achievement
Significance and Impact
Research Details
The work performed at High Flux Isotope Reactor’s HB-2A and HB-3A instruments, Oak Ridge National Laboratory was sponsored by the Scientific User Facilities Division, Office of Basic Energy Sciences, U.S. Department of Energy.
Tan, X., Yaroslavtsev, A., Cao, H., Geondzhian, A., Menushenkov, A., Chernikov, R., Nataf, L., Garlea, O.V., Shatruk, M., Controlling magnetic ordering in Ca1–xEuxCo2As2 by chemical compression. Chemistry of Materials 28, 7459–7469 (2016).
Controlling Magnetic Order by Chemical Compression
Magnetic properties of Ca1–xEuxCo2As2 vary from itinerant (3d) antiferromagnetism of Co in CaCo2As2 to the combination of itinerant (3d, Co) and localized (4f, Eu) ferromagnetism in the intermediate range to localized (4f) antiferromagnetism in Eu-rich samples.
This work demonstrates diverse mechanisms of magnetic ordering in the CaCo2As2–EuCo2As2 realized by chemical compression. This concept can be applied to vary properties of other itinerant magnets guided by theoretical predictions.
The magnetic ground states of Ca1–xEuxCo2As2 were determined by neutron diffraction.
The chemical compression of Eu sites leads to mixed valence that was confirmed by XANES and XMCD.
The changes in the crystal structure and magnetism were justified by band structure calculations.