## Slide 1: Slater Insulator discovered in a new Iridate Perovskite
Scientific Achievement
The magnetism, structural behavior and resistivity change in SrIr1−xSnxO3 indicated this material was a Slater insulator. This is a rare insulator where the magnetism controls the conduction of electrons. The behavior can be controlled by altering the Sn content.
Significance and Impact
There are varies mechanisms that a material can be changed from metallic to insulating, however they are generally independent of magnetism. The Slater mechanism, however, involves the coupling of magnetic order with the insulating behavior. This offers both insights into the fundamental interaction of correlated electrons in compounds and more broadly could provide new routes to devices in the emergent field of spintronics.
Research Details
  Neutron powder diffraction at the HB-2A and HB-3 instruments at the High Flux Isotope reactor confirmed the magnetic ordering and structure.
  Detailed bulk measurements and x-ray measurements were performed to characterize the behavior.
  Work at ORNL’s High Flux Isotope reactor was supported by the scientific User Facilities Division, Office of Basic Energy Sciences, U.S. Department of Energy (DOE
a Neutron diffraction measured magnetic reflections showing long range magnetic order. b Neutron powder diffraction followed the change in crystal structure with Sn substitution. c The proposed magnetic order. The magnetism and control of structure with Sn doping controls the metal-insulator transion.
Q. Cui, J.-G. Cheng, W. Fan, A. E. Taylor, S. Calder, M. A. McGuire, J.-Q. Yan, D. Meyers, X. Li, Y. Q. Cai, Y. Y. Jiao, Y. Choi, D. Haskel, H. Gotou, Y. Uwatoko, J. Chakhalian, A. D. Christianson, S. Yunoki, J. B. Goodenough, and J.-S. Zhou, “Slater Insulator in Iridate Perovskites with Strong Spin-Orbit Coupling” Physical Review Letters 117, 176603 (2016)
a
c
b