## Slide 1: Rare magnetic order and insulating behavior in a 4d oxide
Scientific Achievement
A rare case of magnetic insulating behavior driven by spin-orbit coupling is revealed in the 4d oxide Sr4RhO6.
Significance and Impact
5d oxides can host exotic magnetic and electronic properties driven by an atomic interaction often ignored, but enhanced in 5d systems: spin-orbit coupling (SOC). The influence of appreciable but reduced SOC in 4d oxides is less clear, with one hurdle being the existence of magnetic insulating 4d oxides. Sr4RhO6 was suggested to be the first magnetically ordered 4d rhodate in 1975. Here, we showed magnetic ordering does occur and uncovered the magnetic structure. Combining both experimental and theoretical results we showed Sr4RhO6 to be the first 4d-based oxide that has a magnetical insulating ground state driven by SOC.
Research Details
  Magnetic structure measured with neutron powder diffraction.
  Bulk characterizations showed Sr4RhO6 is an insulator.
  X-ray spectroscopy revealed enhanced SOC behavior.
  Theoretical calculations at ORNL supported the findings.
  The research conducted at ORNL's High Flux Isotope Reactor was sponsored by the Scientific User Facilities Division, Office of Basic Energy Sciences, US Department of Energy. Part of the research was supported by the U.S. Department of Energy, Office of Science, Basic Energy Sciences, Materials Sciences and Engineering Division. Use of the Advanced Photon Source, an Office of Science User Facility operated for the U.S. DOE Office of Science by Argonne National Laboratory, was supported by the U.S. DOE under Contract No. DE-AC02-06CH11357. Experiments were performed at the ORNL High Flux isotopes Reactor’s HB-2A and HB-1A instruments.
Neutron powder diffraction measurements (left) revealed several magnetic Bragg peaks and allowed the magnetic structure to be uncovered (right). Moreover the neutron measurements showed this material to have a crystal structure well-suited to hosting SOC enhanced behavior. Therefore despite a reduced magnitude, relative to 5d oxides, Sr4RhO6 host a magnetic insulating ground state driven by spin-orbit coupling.
S. Calder, L. Li, S. Okamoto, Y. Choi, R. Mukherjee, D. Haskel and D. Mandrus, Physical Review B:Rapid Communication 92 180413(R) (2015). Editors’ Suggestion.