## Slide 1: Atomic Pair Distribution Function (PDF) Analysis 2017 Neutron and X-ray Scattering School
Katharine Page
Advanced Diffraction Group
Chemical and Engineering Materials Division Oak Ridge National Laboratory
pagekl@ornl.gov

## Slide 2: About Me
Advanced Diffraction Group
Group Leader: Matthew Tucker
Tedi-Marie Usher, Katharine Page,
Daniel Olds, and Jue Liu
Spallation Neutron Source,
Oak Ridge National Laboratory
BES Early Career Research Program
BES Scientific User Facility Division
BS in Chemical Engineering University of Maine, 2004
PhD in Materials, UC Santa Barbara, 2008
Director’s Postdoctoral Fellow, Los Alamos National Laboratory (LANL), 2009/2010
Scientist, Lujan Neutron Scattering Center, LANL 2011-2014
Scientist, Chemical and Engineering Materials Division, Oak Ridge National Laboratory (ORNL), 2014-present
2008 Olympic Trials

## Slide 3: What is a local structure?
  Disordered materials: The interesting properties are often governed by the defects or local structure
  Non crystalline materials: Amorphous solids and polymers
  Nanostructures: Well defined local structure, but long-range order limited to few nanometers (poorly defined Bragg peaks)
S.J.L. Billinge and I. Levin, The Problem with Determining Atomic Structure at the Nanoscale, Science 316, 561 (2007).

## Slide 4: What is total scattering?
Cross section of 50x50x50 unit cell model crystal
consisting of 70% blue atoms and 30% vacancies.
Properties might depend on vacancy ordering!
Courtesy of Thomas Proffen

## Slide 5: Bragg peaks are “blind”
Bragg scattering: Information about the average structure, e.g. average positions, displacement parameters and occupancies.

## Slide 6: How about powder diffraction?
Courtesy of Thomas Proffen

## Slide 7: The Pair Distribution Function
  The PDF is the Sine-Fourier transform of the total scattering (Bragg and diffuse) diffraction pattern
Th. Proffen, Analysis of occupational and displacive disorder using the atomic pair distribution function: a systematic investigation, Z. Krist, 215, 661 (2000).

## Slide 8: What is a PDF?
5.11Å
4.92Å
4.26Å
3.76Å
2.84Å
2.46Å
1.42Å
The Pair Distribution Function (PDF) gives the probability of finding an atom at a distance “r” from a given atom.

## Slide 9: Pair Distribution Function
Sine-Fourier transform of all scattered neutron/X-ray intensity (crystalline and amorphous)
Experimental, ensemble, real-space, atom-atom histogram

## Slide 10: Pair Distribution Function
Particle size / correlation length scale
Inter-atomic distances
Number of next-near
neighbors (area under peak)
PDF analysis  Average and short-range structure for disordered crystalline materials, nanomaterials, and amorphous materials

## Slide 11: Pair Distribution Function
Particle size / correlation length scale
Inter-atomic distances
Number of next-near
neighbors (area under peak)
Atom positions
Atomic displacements
Chemical order
Chemical composition
Correlation length scale
Quantitative analysis: fitting a model to the data over specific ranges

## Slide 12: Partial PDFs
s(s+1)/2 partial structure factors characterize a system containing s species
Neutron and x-ray PDFs are often highly complementary!
SrTiO3
Neutron
X-ray

## Slide 13: What types of studies can be done with the PDF technique?

## Slide 14: Local distortions via PDF
Local dipoles
Local Jahn-Teller distortions
Frustrated lattices
etc.
D. Louca, et al., Suppression of superconductivity in Fe pnictides by annealing; a reverse effect to pressure, Phys. Rev. B 84, 054522 (2011).
E. Bozin, et al., Entropically Stabilized Local Dipole Formation in Lead Chalcogenides, Science 330, 1660 (2010).
D. P. Shoemaker, et al., Reverse Monte Carlo neutron scattering study of the 'ordered-ice' oxide pyrochlore Pb2Ru2O6.5, J. Phys.: Condens. Matter 23 (2011).

## Slide 15: Chemical Short Range order via PDF
cis
trans
K. Page, et al., Local atomic ordering in BaTaO2N studied by neutron pair distribution function analysis and density functional theory, Chem. Mater. 19 (2007) 4037-4042.
D. P. Shoemaker, J. Li, and R. Seshadri, Unraveling Atomic Positions in an Oxide Spinel with Two Jahn-Teller Ions: Local Structure Investigation of CuMn2O4, J. Am. Chem. Soc. 131, 11450 (2009).
Substitution effects
Chemical clustering
Ion-specific local environments
Vacancy ordering
Th. Proffen, V. Petkov, S. J. L. Billinge, and T. Vogt, Chemical short range order obtained from the atomic pair distribution function, Z. Kristallogr. 217, (2002) 47–50.
Cu3Au
L.R. Owen, H.Y. Playford, H.J. Stone and M.G. Tucker, Analysis of short-range order in Cu3Au using X-ray pair distribution functions. Acta Materialia (2017) 125, 15-26.

## Slide 16: Nanomaterial structure via PDF
K. Page, Th. Proffen, M. Niederberger, and R. Seshadri, Probing local dipoles and ligand structure in BaTiO3 nanoparticles, Chem. Mater. 22 (2010), 43864391.
Finite size/shape effects
Surface/Interface structure
Nanostructure polymorphs
Growth and transformation
K. W. Chapman, P. J. Chupas, and T. M. Nenoff, Radioactive Iodine Capture in Silver-Containing Mordenites through Nanoscale Silver Iodide Formation, J. Am. Chem. Soc. 132, 8897 (2010).
J. Liu et al, Quantitative analysis of the morphology of {101} and {001} faceted anatase TiO2 nanocrystals, Chem. Mater.

## Slide 17: Amorphous structures via PDF
Kim, H.; Proffen, T.; Chupas, P. J.; Karkamkar, A.; Hess, N. J.; Autrey, T., Determination of structure and phase transition of light element nanocomposites in mesoporous silica: case study of NH3BH3 in MCM-41, J. Am. Chem. Soc. 2009, 131(38) 13749-13755.
Glasses
Liquids
Concretes
Adsorbed gases
etc.
S. Lan, X.. Wei, J. Zhou, Z. Lu, X. Wu, M. Feygenson, J. Neuefeind, X. Wang, In situ study of crystallization kinetics in ternary bulk metallic glass alloys with different glass forming abilities, Applied Physics Letters, 105 (2014) 201906.
H.-W. Wang; L. L. Daemen, M. C. Cheshire, M. K. Kidder, A. G. Stack, L. F. Allard, J. Neuefeind, D. Olds, J. Liu, and K. Page, Synthesis and structure of synthetically pure and deuterated amorphous (basic) calcium carbonates, Chem. Commun., 2017.
Notes: Example: Ammonia borane (AB) in mesoporous silica

## Slide 18: Example: Local structure in BaTiO3
BaTiO3: Ferroelectric oxide, a rhombohedral (R3m) ground state and a room temperature tetragonal (P4mm) structure
Displays order-disorder phenomena: room temperature local structure known to have rhombohedral pair-pair correlations

## Slide 19: Example: Local structure in BaTiO3
BaTiO3: At room temperature, locally has a split (R3m) first Ti-O peak, displaying classic order-disorder behavior
K. Page, T. Kolodiazhnyi, T. Proffen, A. K. Cheetham, and R. Seshadri,, Phys. Rev. Lett. 101, 205502 (2008).

## Slide 20: Example: High Voltage Spinel Cathode LiNi0.5Mn1.5O4
High operating voltage (~4.7 V versus Li+/Li) and facile three dimensional lithium ionic conductivity Zhong et al., 1997; Ohzuku et al., 1999
Two distinct polymorphs are known: Ni/Mn cation ordering strongly impacts electrochemical performance Idemoto et al., 2003; Zhong et al., 1997
  (1) Disordered phase (S.G. Fd-3m), where Ni/Mn are randomly distributed at the 16d site via high temperature solid state reaction
  (2) Long-range cation ordered phase (S.G. P4332 or P4132) via extended post-annealing at 700 °C to 600 °C
Kunduraci & Amatucci, 2006; Kunduraci et al., 2006; Kim et al., 2004; Ma et al., 2010; Moorhead-Rosenberg et al., 2015
Nature of the cation ordering and detailed mechanisms are still debated

## Slide 21: Example: High Voltage Spinel Cathode
Ni/Mn ordering: large nuclear scattering length contrast between nickel (b = 10.3 fm) and manganese (b = -3.73 fm).
Moorhead-Rosenberg, Z., Huq, A., Goodenough, J. B. & Manthiram, A. Electronic and Electrochemical Properties of Li1–xMn1.5Ni0.5O4 Spinel Cathodes As a Function of Lithium Content and Cation Ordering, Chem. Mater. 27, 6934-6945, 2015.
Cation ordering examined at the POWGEN Beamline, SNS
Slow Cooled (SC): 8 hours at 900°C, 1.5°C/min cooling
Fast Cooled (FC): 8 hours at 900°C, 5°C/min cooling
Annealed (A48): 48 hours at 700°C
Annealed (A240): 240 hours at 700°C

## Slide 22: We can tell a lot by looking at PDF data
Local atomic structures almost identical up to 5 Å (two nearest B-site neighbors)
Sample structures diverge after that
Annealed samples: two distinguishable sets of Ni/Mn pairs at third nearest Ni/Mn neighbor distance
By fourth nearest Ni/Mn neighbor samples are very distinct
J. Liu, A. Huq, Z. Moorhead-Rosenberg, A. Manthiram, and K. Page, Nanoscale Ni/Mn ordering in the high voltage spinel cathode LiNi0.5Mn1.5O4, Chemistry of Materials, 28, 19, 6817–6821, 2016.
POWGEN: 3 hours per frame, Q-range: 1 – 30 Å-1
ordered LiNi0.5Mn1.5O4 (S.G. P4332)

## Slide 23: Example: High Voltage Spinel Cathode
The first 10 Å of the non-annealed sample data (FC and SC) differ strongly from long-range structures crystallographic structures
The local atomic structures of the annealed samples (A48 and A240) are well-described by the long-range crystallographic structures
Modeling the local structure with average structure models determined from Rietveld refinement
J. Liu, A. Huq, Z. Moorhead-Rosenberg, A. Manthiram, and K. Page, Nanoscale Ni/Mn ordering in the high voltage spinel cathode LiNi0.5Mn1.5O4, Chemistry of Materials, 28, 19, 6817–6821, 2016.

## Slide 24: Example: High Voltage Spinel Cathode
Least squares refinements of the ordered structure model (P4332) were carried out in a manner that 4b site (Ni site) and 12d site (Mn site) occupancies are allowed to refine simultaneously but with site multiplicity constraints
Over 1 to 5 Å range the ordered models (P4332) with Mn/Ni site mixing provide much better fits for local PDF profiles
Ni/Mn are locally well-ordered in the long-range “disordered” samples
But up to what length scale?
J. Liu, A. Huq, Z. Moorhead-Rosenberg, A. Manthiram, and K. Page, Nanoscale Ni/Mn ordering in the high voltage spinel cathode LiNi0.5Mn1.5O4, Chemistry of Materials, 28, 19, 6817–6821, 2016.
Modeling the local structure with alternate models

## Slide 25: Example: High Voltage Spinel Cathode
5% site mixing in the A48 and A240 patterns throughout the entire range
FC and SC samples are nearly fully disordered at pair distances beyond 15.5 Å
fully ordered
fully disordered
Fit the PDFs within a 4.5 Å “box” in 1 Å steps (a “box-car” refinement)
Spinel cathode materials are distinguished by their unique correlation length scales for chemical short range ordering

## Slide 26: Example: SnO2 Nanocrystals
~2 nm SnO2 (cassiterite) nanocrystals capped with H2O/OH or D2O/OD groups
TGA suggests 2 steps dehydration.
How many layers of water are at the surface?
How is water bonded to surfaces?
What are the dynamics of dehydration?
H.-W. Wang, D. J. Wesolowski, T. Proffen, L. Vlcek, W. Wang, L. F. Allard, A. I. Kolesnikov, M. Feygenson, L. M. Anovitz, and R. L. Paul, Structure and stability of SnO2 nanocrystals and surface-bound water species, J. Am. Chem. Soc., 135, 6885-6895, 2013.

## Slide 27: In situ Dehydration at NOMAD, SNS
Starting with full coverage
Blue lines: 22 and 50 ºC - L1 +L2 +L3
Green lines: 50 to 350 ºC (with 50 ºC increments) - L1 +L2
Black lines: 400 to 850 ºC ( with 50 ºC increments) – SnO2 grain growth
22 oC
850 oC
H.W. Wang, et al, J. Am. Chem. Soc., 2013, 135 , 6885–6895.
Example: SnO2 Nanocrystals

## Slide 28
MD and PDF
MD: hydration layer only
L1 +L2 +L3 : 41 x 41 x 8 Å3
L1 +L2 : 41 x 41 x 6 Å3
L1 : 41 x 41 x 2.5 Å3
Data is compared to Molecular Dynamics Simulation PDFs for nonhydroxylated and hydroxylated models:
Box size: 41 x 41 x 23 Å3 ; 2592 atoms; # density = 0.068 Å-3; Uiso = 0.003 Å2
MD: SnO2 + hyd. layer (hydroxylated model)
0.068
2
1
Observed PDF
0.068
0.084
1
3
4
5
6
7
8
9

## Slide 29
Single phase model:
SnO2 bulk structure, refined particle size = ~47 Å
L1 +L2 +L3
L1 +L2
L1 +0.5L2
Rw : 0.45
Rw : 0.25
Rw : 0.23
L1 +L2 +L3
L1 +L2
L1 +0.5L2
Rw : 0.25
Rw : 0.20
Rw : 0.20
Two phase model: SnO2 bulk + layered MD water structure
Example: SnO2 Nanocrystals

## Slide 30
L1 +L2 +L3
L1 +L2
L1 +0.5L2
L1
H.-W. Wang, D. J. Wesolowski, T. Proffen, L. Vlcek, W. Wang, L. F. Allard, A. I. Kolesnikov, M. Feygenson, L. M. Anovitz, and R. L. Paul, Structure and stability of SnO2 nanocrystals and surface-bound water species, J. Am. Chem. Soc., 135, 6885-6895, 2013.
Example: SnO2 Nanocrystals

## Slide 31: A Few Experimental Considerations

## Slide 32: Total Scattering Structure Function
Structure function, determined from the scattering intensity/differential cross section:
coherent scattering
intensity (corrected)
scattering length (neutrons) or atomic form factor (x-rays)
Corrected for: Container & background scattering, self-absorption, etc.
Normalized by: Incident flux, number of atoms, square of the scattering length/form factor
For unambiguous derivation of this derivation and relationship to other forms:
C. Farrow and S. J. L. Billinge, Acta Cryst. (2009) A65, 232–239.
D. A. Keen, J. Appl. Cryst. 34 (2001) 172-177.

## Slide 33: The Experimental PDF
The total scattering structure factor: S(Q)
The Pair Distribution Function (PDF): G(r)
Sine Fourier transform
The Sine Fourier transform of the total (Bragg and diffuse) scattering

## Slide 34: Obtaining High Quality PDFs
Synchrotron sources or Spallation Neutron Sources
(high energy X-rays) (reactor neutron energies are too low)
High maximum momentum transfer (Qmax)
(2) Good Q-resolution, dQ
(3) Good counting statistics
(4) Low (and stable) instrument background
An ideal measurement would have no contribution from the instrument resolution
For PDF: a wide Q range and high flux is balanced with resolution

## Slide 35: Resolution Effect
Reciprocal space: Peak width, dQ
Real space: Damping with r
Courtesy of
Phil Chater,
Diamond Light Source

## Slide 36: Qmax Effect
Δr resolution of a PDF is dominated by Qmax
  Q = 2π/d = 4πsinθ/λ
  Δr ≈ 2π/Qmax
  Resolution is Qmax limited unless
Cu Kα1, Qmax 8 Å−1
Mo Kα1, Qmax 17.4 Å−1
Ag Kα1, Qmax 22.1 Å−1
Qmax 25 Å−1
Qmax 30 Å−1
Qmax 35 Å−1
AlPO4
B. H. Toby and T. Egami, Acta Cryst. A, 48 (1992) 336
Courtesy of
Phil Chater,
Diamond Light Source

## Slide 37: Instruments at SNS for PDF studies

## Slide 38: Total Scattering at the SNS
NOMAD data collected on 100 mg of sample in a 3 mm quartz capillary in 3 hours.
POWGEN data collected on 10 g of sample in a 10 mm vanadium canister in 12 hours.
high intensity diffraction and PDF for small samples and in situ studies on amorphous, nanostructured, and crystalline materials
high resolution diffraction and PDF of crystalline materials
Pair Distribution Function (PDF) methods follow local atomic bonding configurations, intermediate structure, and correlation length scale- regardless of a material’s long range structure

## Slide 39: Synchrotron Total Scattering: 2D Amorphous Si Detector
P. J. Chupas, K. W. Chapman, P. L. Lee, Applications of an amorphous silicon-based area detector for high resolution, high sensitivity and fast time-resolved pair distribution function measurements, J. Appl. Crystallogr. 40, 463, 2007. http://dx.doi.org/10.1107/S0021889807007856

## Slide 40: Modeling a PDF

## Slide 41: Pair Distribution Function
Atomic PDF (PDFFIT notation):
average density
sum over all atoms
atomic form factors
(Z for x-rays, b for neutrons)
S.J.L Billinge, Z. Kristallogr. Suppl.,26,17 (2007)
distance between i and j atoms
Based on the radial distribution function (RDF):

## Slide 42: Calculating a PDF from a Model
Calculating a PDF from an atomistic model:
Peak Width
  Small model: convolution of (r-rij) with distribution function (PDFgui & TOPAS v6)
  Large model: ensemble average of actual displacements (RMCprofile)
Termination ripples + instrumental dampening
  Multiplication with step function in reciprocal space gives convolution with sin(Qmaxr)/r in real space
  …

## Slide 43: Atomic PDF Modeling
Small Models: Least Squares Refinement
Up to several hundred atoms
‘Rietveld’-type parameters: lattice parameters, atomic positions, displacement parameters, etc.
Refinements as function of r-range
Large Model: Reverse Monte Carlo
20000 + atoms
Fit X-ray and neutron F(Q), G(r) , Bragg profile
Constraints utilized
Static 3-D model of the structure (a snap-shot)
Multi-level / Complex Modeling
Refine higher level parameters (not each atom)
Example nanoparticle: diameter, layer spacing, stacking fault probability
Choose minimization scheme
Emerging: ab initio and force-field based approaches
Density Functional Theory
Molecular Dynamics
PDFgui: http://www.diffpy.org/
Topas V6: http://www.topas-academic.net
RMCprofile: http://www.isis.rl.ac.uk/RMC
EPSR: http://disordmat.moonfruit.com/
DIFFEV and DISCUS: http://discus.sourceforge.net
Topas V6: http://www.topas-academic.net

## Slide 44: Small Box: Software Comparison
PDFgui
+ Open Source and Free
+ GUI is Simple and User-friendly
- Slow refinement, especially for high-r
- No longer actively developed
TOPAS PDF
+ Super Fast
+ Flexible
+ Fit Bragg and PDF together
- Steeper learning curve
- Have to write your own macro
http://www.diffpy.org/
http://www.topas-academic.net

## Slide 45: Large Box: Reverse Monte Carlo
RMCprofile
  Atomic configurations ~600 to 20000+ atoms
  Fit both X-ray and neutron F(Q)
  Fit G(r)
  Fit Bragg profile (GSAS ToF 1-3)
  Polyhedral restraints
  Coordination constraints
  Closest approach constraints
Produce a static 3-D model of the structure (a snap-shot in time)
Link: http://www.isis.rl.ac.uk/RMC

## Slide 46: A Few Emerging Areas

## Slide 47: Magnetic PDF: mPDF
B. A. Frandsen, X. Yang, and S. J. L. Billinge, Magnetic pair distribution function analysis of local magnetic correlations Acta Cryst. A 70, 3–11, 2014.
B. A. Frandsen and S. J. L. Billinge Magnetic structure determination from the magnetic pair distribution function (mPDF): ground state of MnO, Acta Cryst. A, 3, 325-334, 2015.
A. L. Goodwin, M. G. Tucker, M. T. Dove, and D. A. Keen, Magnetic structure of MnO at 10 k from total neutron scattering data, Phys. Rev. Lett. 96, 047209, 2006.
J. A. M. Paddison and A. L. Goodwin, Empirical magnetic structure solution of frustrated spin systems, Phys. Rev. Lett. 108, 017204, 2012.
Being developed to provide direct access to long-range and short-range magnetic correlations in real space
Spin order in diluted magnetic semiconductors, spin-stripe correlations in cuprate superconductors, spin fluctuations in frustrated magnetic systems, etc.

## Slide 48: Field-Dependent PDF
E
Q
η
Q within
10° E
Q within
10° || E
X-rays
X-ray total scattering measured while static electric fields (0 to ~4 kV/mm) are applied to Na½Bi½TiO3 polycrystalline ceramic samples
Bi3+ reorientation observed at high electric field
T.-M. Usher, I. Levin, J.E. Daniels, and J.L. Jones, Scientific Reports 5, 14678 (2015)
11-ID-B, APS

## Slide 49: When Should You Pursue PDF Studies of a Crystalline Material?
You have modeled everything you can in reciprocal space
You suspect the local structure may differ from the long-range structure
Why Would You Suspect a Distinct Local Structure?
Maybe…
You find signatures of disorder through complementary methods
An average structure model fails to explain observed material properties
A theoretical study proposes an alternate structure to the one globally observed
Lots of experience with a materials family or structural archetype

## Slide 50: Some Resources and Programs
Data Collection
Data Extraction
PDFgetN: http://pdfgetn.sourceforge.net
PDFgetX2/X3: http://www.pa.msu.edu/cmp/billinge-group/programs/PDFgetX2/ http://www.diffpy.org/products/pdfgetx3.html
Data Modeling
PDFgui: http://www.diffpy.org/
RMCprofile: http://www.isis.rl.ac.uk/RMC
DISCUS/DIFFEV: http://discus.sourceforge.net
Neutron: http://neutronsources.org
Gudrun: http://disordmat.moonfruit.com/
EPSR: http://disordmat.moonfruit.com/
Topas Academic: http://www.topas-academic.net
ADDIE: ADvanced DIffraction Environment: coming soon from ORNL!
X-ray: http://www.lightsources.org

## Slide 51: References & Reviews
S.J.L. Billinge and I. Levin, The Problem with Determining Atomic Structure at the Nanoscale, Science 316, 561 (2007). http://dx.doi.rog/10.1126/science.1135080
T. Egami and S. J. L. Billinge, Underneath the Bragg peaks: structural analysis of complex materials, Pergamon Press Elsevier, Oxford, England, 2003.
D. A. Keen, Derivation of commonly used functions for the pair distribution function, technique J. Appl. Cryst. 34 (2001) 172-177.
R. Neder and Th. Proffen, Diffuse Scattering and Defect Structure Simulation, Oxford University Press, 2008.
M. G. Tucker, M. T. Dove, and D. A. Keen, Application of the reverse Monte Carlo method to crystalline materials, J. Appl. Cryst. 34, 630-638 (2001).
D. A. Keen and A. L. Goodwin, The crystallography of correlated disorder, Nature 521, 303–309, 2015. http://dx.doi.org/10.1038/nature14453
H. Y. Playford, L. R. Owen, I. Levin, and M. G. Tucker, New insights into complex materials using Reverse Monte Carlo modeling, Annual Review of Materials Research, 44, 429-449, 2014. http://dx.doi.org/10.1146/annurev-matsci-071312-121712

## Slide 52: Summary
Atomic PDF from total (Bragg and diffuse) scattering data gives access to:
Amorphous and nanomaterial structure
Departure from long range (average structure)
  Displacements
  Chemical short range order
  Interstitials/vacancies
Correlation length scale of features (size)
Structure  property relationships
Use multiple data sets (e.g. x-ray and neutron data, diffraction and PDF) to characterize complex materials
High-resolution instruments open the door to medium-range order investigations

## Slide 53: Questions?
pagekl@ornl.gov